Glaze Recipe and Test Notes

Wilson Ceramics   |   208 Capitol Street   |   Charleston WV   |   Cone 6 Electric

## Linen Satin Matte (LSM-01)

Base type: Satin matte   |   Fire range: Cone 6 electric   |   Status: Production glaze - current palette

| Ingredient | Grams | Percent |
| --- | --- | --- |
| Custer Feldspar | 1500 | 37.5% |
| Silica (325 mesh) | 900 | 22.5% |
| Whiting | 700 | 17.5% |
| EPK Kaolin | 500 | 12.5% |
| Talc | 250 | 6.2% |
| Zinc Oxide | 150 | 3.8% |
| TOTAL | 4000 | 100.0% |

Mixing notes: Batch at 5000g. Sieve 80 mesh twice. Apply 3 coats dip or 4 layers brush. Wax foot ring.

Surface: Satin matte, smooth, low sheen

Color oxidation: Warm off-white, slight cream warmth

Movement: None to very slight - good for plates

Dishwasher safe: Yes - vitrified at cone 6

Notes: Primary glaze for commission work. Matches well with clay body 1183 (Highwater). No crawling observed in 40+ firings. Consistent piece to piece.

## Satin Amber (SA-03)

Base type: Satin matte with iron   |   Fire range: Cone 6 electric   |   Status: Production glaze - current palette

| Ingredient | Grams | Percent |
| --- | --- | --- |
| Custer Feldspar | 1200 | 35.3% |
| Silica (325 mesh) | 700 | 20.6% |
| Whiting | 600 | 17.6% |
| EPK Kaolin | 400 | 11.8% |
| Talc | 200 | 5.9% |
| Zinc Oxide | 100 | 2.9% |
| Red Iron Oxide | 120 | 3.5% |
| Rutile | 80 | 2.4% |
| TOTAL | 3400 | 100.0% |

Mixing notes: Batch at 3000g. 80 mesh. Apply 3 thin dip coats. Avoid over-application - will run at cone 6 if thick.

Surface: Satin, slight texture from rutile, warm

Color oxidation: Warm amber to ochre, variation with layer thickness

Movement: Slight breaking on rims, controlled

Notes: Best on mugs and bowls where rim break reads as character. Iron content varies by supplier - retest with new RIO batches.

## Celadon Grey Gloss (CGG-02)

Base type: Clear gloss with iron and titanium   |   Fire range: Cone 6 electric   |   Status: Production glaze - current palette

| Ingredient | Grams | Percent |
| --- | --- | --- |
| Custer Feldspar | 1400 | 38.5% |
| Silica (325 mesh) | 1100 | 30.2% |
| Whiting | 700 | 19.2% |
| EPK Kaolin | 300 | 8.2% |
| Zinc Oxide | 50 | 1.4% |
| Red Iron Oxide | 30 | 0.8% |
| Titanium Dioxide | 50 | 1.4% |
| Cobalt Carbonate | 8 | 0.2% |
| TOTAL | 3638 | 100.0% |

Mixing notes: Batch at 3000g. 100 mesh sieve. Apply 2 coats dip - thinner than matte glazes. No wax needed.

Surface: Gloss, fluid surface, slight blue-grey warmth

Color oxidation: Cool grey to celadon blue depending on thickness

Movement: Slight pooling in bowl bottoms - intentional

Notes: Cobalt content is low - increase to 15g for a more pronounced blue shift. Works best on pieces with interior curves where pooling can collect.

## Sage Green Matte (SGM-04)

Base type: Satin matte with copper and chromium   |   Fire range: Cone 6 electric   |   Status: Production glaze - current palette

| Ingredient | Grams | Percent |
| --- | --- | --- |
| Custer Feldspar | 1300 | 37.4% |
| Silica (325 mesh) | 800 | 23.0% |
| Whiting | 650 | 18.7% |
| EPK Kaolin | 450 | 12.9% |
| Talc | 220 | 6.3% |
| Copper Carbonate | 40 | 1.2% |
| Chrome Oxide | 15 | 0.4% |
| TOTAL | 3475 | 100.0% |

Mixing notes: Batch at 3000g. 80 mesh. Apply 3 coats dip. Test all copper/chrome glazes with tile - slight formula variations matter.

Surface: Satin matte, slightly dry texture

Color oxidation: Sage green, variation to olive depending on kiln position

Movement: None

Notes: Chrome-copper glazes are volatile. Do not fire with glazes containing RIO in the same load - can cause color contamination from atmosphere. Load separately on a kiln shelf.

## Rust Red Matte (RRM-05 - EXPERIMENTAL)

Base type: Matte with high iron   |   Fire range: Cone 6 electric   |   Status: Testing - 4 tile tests to date

| Ingredient | Grams | Percent |
| --- | --- | --- |
| Custer Feldspar | 800 | 32.5% |
| Silica (325 mesh) | 500 | 20.3% |
| Whiting | 500 | 20.3% |
| EPK Kaolin | 350 | 14.2% |
| Red Iron Oxide | 250 | 10.2% |
| Manganese Dioxide | 60 | 2.4% |
| TOTAL | 2460 | 100.0% |

Mixing notes: Batch at 2000g test only. 80 mesh. Apply medium - thick application turns brown, thin turns orange. Variable.

Surface: Dry matte to satin depending on application

Color oxidation: Rust to terra cotta - high variability

Movement: Some running at heavy application

Notes: Promising but inconsistent. Try reducing MnO2 to 30g on next test. Not recommended for production work until 3 successful firings documented. Keep test tiles labeled with date and application thickness.

# General Lab and Mixing Notes

Always sieve twice. First pass breaks up lumps; second pass catches what the first missed.

Specific gravity (SG) targets: matte glazes 1.42-1.48; gloss glazes 1.38-1.44. Check with a hydrometer before application.

Label every test tile with: glaze name, batch date, application method, cone, and firing date. An unlabeled tile is worthless.

Weigh materials in grams on a digital gram scale (0.1g accuracy minimum). Volume measurements are unreliable for chemistry.

Glaze buckets seal with lids - no evaporation between applications. Add water to adjust SG, not more materials.

Fire test tiles in the same kiln and position as production pieces to get useful data.

When a glaze fails: document what happened (crawled, ran, pinholed, color wrong), then adjust one variable at a time.

Batch size: 3000g is a good working batch. 5000g if a glaze is going into heavy production.

Store dry materials in sealed lidded buckets labeled with supplier, material name, and date received.

Wilson Ceramics  |  208 Capitol Street  |  Charleston WV 25301  |  Cone 6 Electric