## Slide 1
Glaze Chemistry and Surface
An introduction for studio ceramics students
ENG-225 Ceramics Studio I | University of Charleston | James A. Wilson

## Slide 2
Why Does Glaze Chemistry Matter?
Understanding glaze lets you solve problems and create intentionally
A glaze that crawls, pinholes, or runs is not bad luck - it is chemistry you can diagnose
Understanding the formula lets you modify an existing recipe rather than starting over
Every glaze you use was designed by someone who understood the triaxial - now you will too
Cone 6 electric has specific chemistry requirements that differ from cone 10 or raku - knowing why matters
Once you understand the structure, you can begin to predict what a recipe will do before you fire it

## Slide 3
The Three Glaze Component Families
Every ingredient in every glaze fits one of three roles
Glass Formers
Create the glass matrix. Silicon dioxide (silica) is the primary glass former. Boron is a secondary glass former used in lower-fire glazes.
Fluxes
Lower the melting temperature. Without flux, most glazes would not melt at any achievable kiln temperature. Common fluxes at cone 6: calcium (whiting), magnesium (talc), sodium, potassium, lithium, zinc.
Stabilizers
Prevent the glaze from running and hold the texture in suspension. Alumina (Al2O3) is the primary stabilizer - introduced through kaolin or feldspar.

## Slide 4
Common Glaze Materials at Cone 6
What you will find in most studio glaze recipes
Material | Role | Notes
Custer Feldspar | Flux + silica + alumina | Most common feldspar in cone 6 glazes; introduces multiple oxides
Silica (325 mesh) | Glass former | Pure SiO2; tightest control of glaze glass
Whiting | Flux (calcium) | Calcium carbonate; burns off CO2 in firing
EPK Kaolin | Stabilizer + alumina | Also adds suspension in wet glaze
Talc | Flux (magnesium) | Small amounts smooth the glaze surface
Zinc Oxide | Flux | Promotes matte surface at moderate amounts
Red Iron Oxide | Colorant | Warm tans to browns to blacks depending on amount and atmosphere
Cobalt Carbonate | Colorant | Strong blue; use 0.5-2% only - very powerful
Copper Carbonate | Colorant | Greens in oxidation; powerful, fugitive
Titanium Dioxide | Opacity + texture | Small amounts create matte and visual texture

## Slide 5
Glaze Surface Types at Cone 6
The glaze surface is a design choice, not a default
Gloss
High silica, adequate flux, low alumina. Fluid surface. Shows movement and pooling. Best: bowls, interior surfaces.
Satin Matte
Balanced silica/alumina, moderate zinc or calcium. Smooth, low sheen. Consistent piece to piece. Best: functional ware, plates.
Dry Matte
High alumina or magnesium, lower silica. Can be dusty or crawl if too thin. Best: textured surfaces, hand-building.
Crystalline
High zinc, special firing schedule. Grows visible crystals during slow cooling. Complex, not for beginners.

## Slide 6
Reading a Glaze Recipe
Linen Satin Matte (LSM-01) - Wilson Ceramics production glaze
Recipe (5000g batch)
Custer Feldspar
1500 g
30.0%
Silica 325 mesh
900 g
18.0%
Whiting
700 g
14.0%
EPK Kaolin
500 g
10.0%
Talc
250 g
5.0%
Zinc Oxide
150 g
3.0%
TOTAL
4000 g
80.0%
What the Recipe Tells Us
Glass formers:
Silica (SiO2)
Primary flux:
Calcium (whiting) + potassium/sodium (feldspar)
Secondary flux:
Magnesium (talc) + zinc oxide
Stabilizer:
Alumina (EPK + feldspar)
Colorants:
None
Surface prediction:
Satin matte, warm off-white, low movement

## Slide 7
Glaze Problem Diagnosis
Failures are data - read them
Problem | Symptom | Likely Cause and Fix
Crawling | Glaze pulls away from surface in lumps during firing | Too thick application, dusty bisqueware, or high clay content shrinking glaze
Pinholing | Small holes remain in fired glaze surface | Outgassing from clay body or contamination; try slower hold at peak temperature
Running | Glaze flows down sides, pools on shelf | Too much flux, too thick, or fired too high. Adjust flux, reduce application, or fire lower
Crawling on edges | Glaze flakes off sharp edges | Sharp edges do not hold glaze; soften edges before glazing
Color not as expected | Fired color differs from recipe | Different supplier batch, SG wrong, application too thin or thick, kiln position difference

## Slide 8
This Week's Lab
Assignment: Mix, Apply, and Test
Mix a batch of Linen Satin Matte (LSM-01) at 500g using the recipe on your handout
Apply it to two test tiles at two different thicknesses - label both
Glaze one cylinder from Project 2 with LSM-01 using the dipping method
Fire the test tiles and cylinder together in the next bisque/glaze cycle
Document your SG measurement and application method on your glaze notes sheet
Questions? Office hours by appointment - james.wilson@ucharleston.edu