## Slide 1
Kiln Firing Report
Kyoto Craft Association

## Slide 2
Firing Summary F-25-11
1
Gas reduction kiln at Higashiyama
Three-day cycle including slow cooling
Targeted cone 10 reduction

## Slide 3
Temperature Notes
2
Even climb to 1080C, then heavy stoking
Back left corner reached cone 9 comfortably
Hold for 30 minutes to develop ash surface

## Slide 4
Glaze Results
3
Celadon pieces showed excellent clarity
Some pooling on the large platters
Tenmoku achieved deep, rich black

## Slide 5
Maintenance Items
4
One cracked bisque shelf needs replacement
Burner ports cleaned post-firing
Thermocouple readings remain within tolerance