## Slide 1
AMERICAN INSTITUTE FOR CONSERVATION
Annual Meeting 2026
Salt Lake City, Utah - November 12, 2026
REVERSIBLE MOUNTING TECHNIQUES FOR HISTORIC TEXTILES
A Practical Framework
Jesse Perez
Perez Textile Conservation Jamaica Plain, Boston, MA
MOUNTING
TECHNIQUES
6
Case Studies
14+
Institutions
2020-26
Practice Years
22
Objects Active

## Slide 2
Jesse Perez | Perez Textile Conservation | Jamaica Plain, Boston
THE CORE PROBLEM
Why Mounting Matters as Much as Treatment
Long-term stability
A mounted textile is under constant, low-level mechanical stress. Poor mount design causes more damage over decades than most treatments.
Reversibility imperative
Every mounting decision must be undoable by a future conservator without damaging the object. Adhesives, fasteners, and substrates that trap are failures.
Exhibition vs. storage tension
Exhibition mounts optimize for visibility. Storage mounts optimize for minimal contact and environmental stability. They often conflict.
Field Observation
"Of the condition failures I have examined on acquisition, roughly half trace to mounting decisions made at installation, not treatment failures in the object itself."

## Slide 3
Jesse Perez | Perez Textile Conservation | Jamaica Plain, Boston
FRAMEWORK
A Four-Principle Mounting Framework
01
No Adhesive to Object
The textile never touches an adhesive material. All attachment is mechanical - stitch-based, gravity-based, or clip-based using reversible, inert materials.
02
Substrate Compatibility
Substrate materials (board, foam, fabric) must be pH-neutral, off-gassing tested, and dimensionally stable across the expected humidity range.
03
Weight Distribution
The mount distributes the object's weight across the maximum possible contact area. No point loading. No edge stress.
04
Future Access
Any conservator must be able to remove the object from the mount in under 30 minutes without cutting, soaking, or mechanical force beyond hand pressure.

## Slide 4
Jesse Perez | Perez Textile Conservation | Jamaica Plain, Boston
MATERIAL SELECTION
Approved Materials by Mounting Application
Material | Application | pH / Stability | Reversibility | Source
Linen, washed & aged | Primary cover for substrate boards | Neutral 7.0 | Full - unstitched | Conservation supply
Hollytex polyester 3256 | Interleaving layer; object face barrier | Inert, pH neutral | Full - peeled | Conservation supply
Dibond aluminum composite | Exhibition backing panel | pH neutral, stable | Full - object unstitched | Fabrication supplier
Ethafoam 25mm | Cushion layer for padded mounts | Inert, no off-gas | Full - cut away | Conservation supply
Paraloid B-72 in ethanol | Local consolidant only, not adhesive to mount | Stable, reversible | Solvent reversible | Lab supplier
Stainless steel pins 0.3mm | Temporary positioning only; removed pre-install | Inert | Full - hand removed | Specialty supplier
Cotton cord, undyed | Stitch attachment in linen pocket method | pH neutral, stable | Full - cut away | Conservation supply

## Slide 5
Jesse Perez | Perez Textile Conservation | Jamaica Plain, Boston
CASE STUDY 01
Ottoman Embroidered Panels - Linen Pocket Method
Six 17th-18th century panels for major Boston museum. Exhibition mount design for December 2026 opening.
1.
Dibond panel covered with washed linen, hand-stitched taut
2.
Hollytex interleaving layer stitched to linen surface
3.
Ottoman panel laid face-up; position marked with conservation pencil
4.
Linen pockets stitched around panel perimeter - no penetration of embroidery
5.
Cotton cord laced through pocket system to distribute tension evenly
6.
Panel weight: 0.8-1.4 kg. Board designed for 3x safety factor.
7.
Full removal possible in under 20 minutes without tools
Panel Specifications
Panel count
6 panels (PTC-2024-031)
Period
17th - 18th century
Dimensions range
48x62 cm to 71x94 cm
Ground fabric
Linen tabby, z-spun
Embroidery
Silk + silver-gilt metallic
Substrate
Dibond 3mm / linen cover
Pocket cord
Cotton, 26/2 nm, undyed
Inst. target
December 2026, MFA Boston
Conservator
Jesse Perez, PTC

## Slide 6
Jesse Perez | Perez Textile Conservation | Jamaica Plain, Boston
CASE STUDY 02
American Samplers - Mat Window Method
22 samplers, 1750-1850 - Peabody Essex Museum. Conservation framing for long-term study access.
Chart: Condition Tiers - 22 Samplers
| Tier A (Urgent) | Tier B (Priority) | Tier C (Stable)
Objects | 7 | 10 | 5
Mat Window Method
4-ply acid-free mat board, window cut to 8mm inside object edge
Hollytex barrier between object face and mat surface
Hinge attachment: Japanese tissue 9g/cm, wheat starch paste
Hinges attach to back mat only - object face untouched
Back board laced with archival cotton tape for lateral support
Removable: hinges soluble in deionized water, <15 min
Storage orientation: horizontal, interleaved with Hollytex

## Slide 7
Jesse Perez | Perez Textile Conservation | Jamaica Plain, Boston
COMPARISON
Reversibility Performance by Method
Method | Object Contact | Removal Time | Tool Required | Risk Level | Best For
Linen Pocket | None to object | 15-20 min | Scissors only | Low | Heavy embroidery, panels
Mat Window + Hinge | Minimal (verso edge) | 10-15 min | Moisture, tweezers | Low | Samplers, flat works
Stitch-to-net | Net overlies face | 20-30 min | Scissors only | Low-medium | Fragile, open weave
Padded Ethafoam | Foam face (Hollytex barrier) | 5-10 min | None | Low | Storage, transit
Legacy: staple to board | Direct penetration | 45+ min, destructive | Pry bar, pliers | HIGH | NEVER use
Legacy: pressure adhesive | Full face contact | Hours, solvent risk | Solvents, scalpel | HIGH | NEVER use

## Slide 8
Jesse Perez | Perez Textile Conservation | Jamaica Plain, Boston
OUTCOMES
Long-Term Stability Tracking - 6 Year Dataset
Objects remounted 2020-2024 (n=34). Annual condition check by fiber survey and environmental log review.
Chart: Damage Events vs. Interventions per Year
| 2020 | 2021 | 2022 | 2023 | 2024 | 2025
New damage events | 0 | 0 | 1 | 0 | 1 | 0
Proactive interventions | 2 | 1 | 1 | 2 | 1 | 1
34
Objects remounted since 2020
0
Adhesive failures
6
Successful removals for treatment
98%
Annual condition checks stable

## Slide 9
Jesse Perez | Perez Textile Conservation | Jamaica Plain, Boston
CONCLUSIONS
Practical Takeaways for Textile Mount Design
01
Never adhere to the object
Stitch-based and pocket methods provide equal or better stability than adhesive, and maintain full reversibility for the next conservator.
02
Specify the removal scenario before installing
A mount designed without a mental model of how it will be undone is a problem deferred, not a problem solved.
03
Document the mount as carefully as the treatment
The mount record must include materials, dimensions, contact points, and removal method. Future conservators need this.
04
Test substrate off-gassing before contact
Especially for long-term storage mounts. Board and foam can release volatiles that affect dye stability over years.

## Slide 10
Thank You
Questions and discussion welcome.
Jesse Perez
Perez Textile Conservation
Jamaica Plain, Boston, MA 02130
(617) 555-3800
jesse.perez@Finthesiss.ai
Specializations
- Latin American textiles
- Ottoman embroideries
- American colonial samplers
Paper text and supplementary material available on request via email.